**Seyer Industries – Chemical Processing Capabilities**

 Seyer Industries is committed to providing our customers with top tier delivery and quality. In efforts to become more vertically integrated, Seyer has installed a state-of-the-art metal finishing line to its core capabilities. Below is a list of specifications and processes Seyer will be able to provide:

* **Anodize**
	+ MIL-A-8625
		- Type IC – Boric Sulfuric
		- Type IIB – Thin Film
* **Conversion Coat**
	+ MIL-DTL-5541
		- Class IA
* **Passivation**
	+ SAE-AMS-2700
		- Type II
		- Type VI
	+ ASTM A 967
		- Type II
		- Type VI
* **Pre-Penetrant Etch**
	+ ASTM E 1417
	+ Per Prime / Customer Specification
* **Aluminum Etch**
	+ Per Prime / Customer Specification
* **Titanium Etch**
	+ Per Prime / Customer Specification
* **Tank Size**
	+ Tank Size: 33” Wide x 60” Long x 60” Deep
	+ Tank Volume: 542 gallons